## Slide 1: MOS capacitor – MOSFET transistor – MOS inverterS
Prof. Philippe LORENZINI
Polytech-Nice Sophia

## Slide 2: Outline
Metal Oxyde Semiconductor Structure
MOS Transistor
MOS Inverters
  NMOS
  CMOS

## Slide 3
Two definitions (only 2!)
  Work Function (Travail de sortie) : this is the energy we have to give to an electron to extract it of metal without kinetic energy. It reaches the "vacuum level". Work function is the energy difference between the vacuum level and the highest occupied energy level, ie the Fermi level.
  Electron Affinity (Affinité électronique ) : it’s the difference between the vacuum level and the bottom of the conduction band. It’s only defined for SC and not for Metal.
  Unity for both of them: eV (electron volt)

## Slide 4: Metal Oxyde Semiconductor Structure
MOS capacitor
Energy band diagram of the three components of a MOS system

## Slide 5: Field Effect Transistor
The field effect is the variation of the conductance of a channel in a semiconductor by the application of an electric field

## Slide 6: Equilibrium of MOS structure
EF
EF
Metal
SC(n)
EV
EC
Independant system
EF
EF
Metal
SC(n)
EV
EC
eVbi
Equilibrium state
dx

## Slide 7: The five regimes : a function of work function
Accumulation
Flat band
Desertion / depletion
Weak inversion
Strong inversion
Ox

## Slide 8: Energy band diagram for ideal n and p type MOS capacitors under different bias conditions

## Slide 10
We suppose we deal with a p type semiconductor:
warning: in few books, absolute value is not present!!!!
Field, potential and charges in Silicon

## Slide 11
Poisson’s Equation:
Charge density
Field, potential and charges in Silicon (p-type)

## Slide 12
Field, potential and charges in Silicon

## Slide 13
We calculate the integral from bulk to a point x in SC
V(x=« bulk »)=0 et
And the Electric Field is given by:
Field, Potential and Charges in Silicon
M
O
S
Vg

## Slide 14
With the Debye length:
If we use the Gauss’s theorem:
Field, potential and charges in Silicon

## Slide 15
With the Debye length:
If we use the Gauss’s theorem:
Field, potential and charges in Silicon
Qsc
X=0
E=0
E=-Es
E=Ex

## Slide 16
For Vs (and so Vg) negative
(accumulation)
For Vs (and Vg) positive but
less than 2Ffi
(depletion – weak inversion)
For Vs (and Vg) > 2Ffi
(strong inversion)
Field, potential and charges in Silicon
Allways negligible (p type)

## Slide 17: Weak / Strong Inversion
  ns=p0=NA
This condition will define a very important parameter of the struture: the threshold voltage or the required gate voltage to put the transistor in strong inversion regime
eFFI

## Slide 18: Measurement of capacitance in Ideal MOS Structure
The C-V curve is usually measured with a CV meter:
We apply a DC bias voltage Vg + small sinusoidal signal (100 Hz to 10 MHz)
We measure the capacitive current with an AC meter (90 degree phase shift) => icap/vac =wC

## Slide 19: Measurement of capacitance in Ideal MOS Structure
When a voltage Vg is applied on the MOS Gate, part of it appears as a potential drop across oxide and the rest of it appears as a band bending Vs in silicon:
M
O
S
Vg
Vox
VSC
Oxide and Silicon have capacitor behavior
VG
VOX
VS
X
V(X)
-tOX
0
SC is grounded,
so VSC=VS

## Slide 20
Oxide capacitance: as a parallel-plate capacitor
We can also write :
Measurement of capacitance in Ideal MOS Structure

## Slide 21: Measurement of capacitance in Ideal MOS Structure
Semiconductor (silicon) capacitance

## Slide 22: Measurement of capacitance in Ideal MOS Structure
Global capacitance of the structure:
If we combine the 3 relations above :
M
O
S
Vg
Vox
VSC

## Slide 23: Measurement of capacitance in Ideal MOS Structure
Total charge QSC depends on different regimes
 2 types of charges, fixed and mobile/free:
Semiconductor capacitance can be written as:

## Slide 24: Measurement of capacitance in Ideal MOS Structure
Semiconductor capacitance can be written as:
Total charge in SC depends on different regimes
 2 types of charges, fixed and mobile/free:

## Slide 25: Measurement of capacitance in Ideal MOS Structure
Summary: MOS capacitor is equivalent :
  of 2 capacitors connected in serie, COX and CSC
  CSC is equivalent of two capacitors
  - the two are variable and be view as 2 capacitors in //
Cox
Csc
Cox
Cs
Cdep
Conclusion: the total capacitance of MOS structure is function of bias conditions or operating regime through CSC

## Slide 26: Capacitance of MOS structure
Accumulation Regime: VS<0 ie VG<0

## Slide 27: Capacitance of MOS structure
Accumulation Regime: VS<0 ie VG<0
Cox
Csc

## Slide 28: Capacitance of MOS structure
Accumulation Regime: VS<0 ie VG<0
kT=26 meV, in accumulation regime VS is around -0,3 V to -0,4 V,  as soon as VG<-1 to -2 V, so we can simplify to:

## Slide 29: Capacitance of MOS structure
Flat Band: VS =0 V ie VG=0 V
(warning : ideal structure!!!!!)
Analytical computing:
<< dox

## Slide 30: Capacitance of MOS structure
Depletion regime and weak inversion
Wdep
Insulator e

## Slide 31: Capacitance of MOS structure
Depletion regime and weak inversion

## Slide 32: Capacitance of MOS structure
Strong inversion

## Slide 33: Capacitance of MOS structure
p type SC
accumulation
dep
???
p type SC
Strong inversion

## Slide 34: Capacitance of MOS structure
Strong inversion:
Which mechanism governs the onset of strong inversion layer?
P type SC : we must create electrons at oxide/SC interface. Where they come from?
  From Metal : NO because oxide barrier
  From SC (neutral region) : NO minority carriers (e-)
Only one solution: thermal (or optical) generation

## Slide 35: Capacitance of MOS structure
Strong inversion:
  Thermal generation?
    #1 :In the space charge + dissipation of charge by electric field
    #2 : In the neutral region
  First mechanism dominates but it’s a slow one.

## Slide 36: Capacitance of MOS structure
Strong inversion
  Which Delay time to create strong inversion layer ?
Strong inversion limit: nS = NA
More realistics
Shockley-Read equation
Si:
ni=1010 cm-3
NA=1015 cm-3 ts=1s !!
tm=10-5 s

## Slide 37: Capacitance of MOS structure
When we measure C(V) , results depend on YES or NO, we give enough time to create this layer
  YES: we measure capacitance du to inversion layer
  NO : Depletion layer preserves the neutrality of the system with an increase of its width . The limit is the breakdown of the semiconductor
Results are frequency dependant

## Slide 38
3 cases :
Low frequency
+
Slow ramp Vg
x
Q
x
Q
High frequency
+
Slow ramp Vg
x
Q
High frequency
+
High ramp Vg
Capacitance of MOS structure:
strong inversion

## Slide 40
minimum capacitance (HF):
BF
HF
Capacitance of MOS structure: strong inversion

## Slide 41: MOS capacitor : parasitic effects
2 factors modify « ideal » structure of MOS capacitor.
  The charges in oxide and/or charges at interface Oxide – SC.
  The difference between the work function of the Metal and the SC
Influence on the threshold voltage VT of the structure.

## Slide 42: MOS capacitor :oxide charge
Distribution of charges in the oxide :
  Mobile ionic charges
  Oxide traped charges
  Fixed oxide charges
  Traped charges at Si-SiO2 interface
K+
Na+
Ionic mobiles
- - - -
+ + + +
traped
+ + + + +
x x x x
SiO2
SiOx
Si
Depending on their position in the oxide, the charges will influence more or less on the electron population below the gate.

## Slide 43: MOS capacitor :oxide charge
Effect of a sheet charge of a real density Q within the oxide layer of an MOS capacitor:
Oxide
x
r(x)
Vg=0V
Si
Metal
0
x1
Q
x
r(x)
Vg=Vfb
dox
-Q
Q
Oxide charges are compensated with charges in Metal AND SC.
If Vg=Vfb, charges in SC must be zero. Only Metal « DO the job »

## Slide 44: MOS capacitor :oxide charge
The effect is maximum when the charges are located at the interface oxide - SC, ie Qox=QSS (and no effect if Qox close to Metal)
It is a common practice to define an equivalent oxide charge per unit area Qox located at the oxide – silicon interface (named QSS):

## Slide 45: Work function difference
Work function difference  non zero oxide field.
  Even when Vg = 0 V, structure show a band bending
eci
Depletion zone
A gate voltage must be applied to restore the flat band condition  VFB = fM – fS = fMS : this voltage is called Flat Band voltage VFB

## Slide 46: Work function difference
Work function difference.
  Example: polysilicon n+ gate on p-MOS

## Slide 47: Non ideal MOS capacitor
Taking into account both Oxide charges and work-function difference, the global flat band voltage can be written as:
Warning: this is the voltage we have to apply on the gate to restore de flat band condition.

## Slide 48
Imagine the depletion regime of the MOS capacitor (Qss=0)
We know that :
Capacitance of Non ideal MOS structure:
~

## Slide 49
Imagine the depletion regime of the MOS capacitor (Qss=0)
We know that :
Capacitance of Non ideal MOS structure:
~

## Slide 50: Threshold voltage
Key parameter for behavior understanding of transistor
Many definitions (same results!):
  nS = NA
  Vs = 2 ffi
  …

## Slide 51: Threshold voltage
VT is simply the applied gate voltage when the surface potential or band bending reaches 2FFI and the silicon charge is equal to the bulk depletion charge for that potential
(we suppose here that no bias on the bulk is present  no body effect)
VT
VOX
VS=2FFI
X
V(X)
-tOX
0
(from slide 17
and 48)

## Slide 52: Threshold voltage
Substrate sensitivity - Body Effect
  In general the MOS devices have a common silicon substrate  substrate voltage is equal for all transistor.
  BUT when multiple NFETs (or PFETs) are connected in series in a circuit, they share a common body (the silicon substrate) but their sources do not have the same voltage. We must introduce a coefficient that accounts for this effect :g

## Slide 53: Threshold voltage
=0
>0
+++++++
<0
>0
+++++++
+ + +
- - -
One part of Gate voltage is no more used to create inversion layer but just to compensate the extra depletion width  VT will increase

## Slide 54: Threshold voltage
The new threshold voltage taking account the body effect can be written as:
The substrate sensitivity as:
Of course substrate bias have to be reverse to prevent current flow

## Slide 55: Threshold voltage
The effect of (reverse) substrate bias is to widen the bulk depletion region and raise the threshold voltage:
The back contact acts as a back Gate
We can tune VT !
0
2
4
6
8
10
0,8
1,0
1,2
1,4
1,6
1,8
Na = 1E16 cm
-3
Na = 3E15 cm
-3
T
Substrate bias voltage
V
SB
(V)
Threshold voltage (V)

## Slide 56
Threshold voltage : body effect
Drawback or advantage ?

## Slide 57: MOS-FET transistor

## Slide 58
MOS-FET transistor

## Slide 59: Graphical summary of the major processing steps in the formation of a MOSFET Transistor
http://www.youtube.com/watch?v=dR-Qtv-7uWI

## Slide 60
MOS-FET transistor
Stockage time ?

## Slide 61: Linear regime

## Slide 62: Saturation / linear limit

## Slide 63: Saturation regime
Effective length of canal decreases from L to L’

## Slide 64: Basic MOSFET IV Model
L, canal length( y oriented)
W, canal width(z oriented)
V, voltage in the canal (f(y))
  V(y=0) = V(source) = Vs = 0 V
  V(y=L) = V (drain) = Vds
Vg, gate voltage
-VBS, body voltage

## Slide 65: Charge sheet approximation
Analytical solution  we simplify the model:
  Charge sheet approximation (xi=0):
    We assume all the inversion charges are located at the silicon interface without any thickness
  No potentiel drop across this layer
  No band bending across this layer

## Slide 66: Charge sheet approximation
First step: calculation of inversion layer charge function of Vg

## Slide 67: Charge sheet approximation
Current density in the channel can be caused by diffusion and drift components
Current is simply given (integration over channel section)
There is a sign change because we want IDS>0 in –y direction

## Slide 68: Charge sheet approximation
The previous relation can be rewritten
If we remember that:
Current expression can be found
And so, by integrationg from y=0 to y=L and as current is independant of y:
conduction
diffusion

## Slide 69: Charge sheet approximation
If we want to derive basic expressions for long channel current in linear and saturation regions, we can neglect drift component
After few simple steps:
!! Cox is the oxide capacitance per surface unit (Fm-2 ou Fcm-2)!!
with

## Slide 70: Characteristics in the linear (triode) region
When VDS is small (VDS << 2FFi) , one can expand the previous equation into power series in VDS and keep only first order term:
We recognize threshold voltage VT.
In the linear region, the MOSFET simply acts like a resistor modulated by the gate voltage

## Slide 71
For larger values of VDS we have to keep second order term (quadratic term) and a good approximation of current is:
Cdm is the bulk depletion capacitance in limit of strong inversion
with
Characteristics in the linear (triode) region

## Slide 72: Characteristics in the saturation region
Previous equation is a parabole. Ids follows a parabolic curve with VDS until a maximun (or saturation) value is reached when VDS = Vdsat.
In the case of thin oxide and low doping m can be reduced to 1 and yield the well known expression:
Drain current
VDS

## Slide 73
Without any approximation (series expand,…), complete expressions for IDSAT can be expressed as:
If we suppose high value for Cox (thin oxyde) and low doping level, threshold voltage can be simplified as , and at the same time we can rewrite
Characteristics in the saturation region

## Slide 74: Subthreshold characteristics – weak inversion region
Three regimes:
  Triode (Linear)
  Saturation
  OFF state (if Vg < VT for nMOS)
Transition ON /OFF is not so sharp
  Weak inversion for Ffi <Vs <2FFi
  Subthreshold behavior is of importance:
    Low power
    Low voltage
digital logic and memory circuits

## Slide 75: MOSFET basics
Subthreshold current : « OFF » is not totally « OFF »
  Previous analysis  VGS<VT, NMOS (NFET) turns OFF
  In reality, for VGS~VT, a « weak » inversion layer still exists and some current (drift component) can flow between S and D.
  This is the so called “subthreshold conduction”
  with , a ideality (or nonideality) factor (≥1)
  Remember that changes by 10 for every x60 mV change in VGS.
  Typically, if IDS decreases for one decade , then VGS must decrease by at least x60 mV (in fact around 80 mV, h > 1) (at 300K!).

## Slide 76: MOSFET basics
Subthreshold current :
(for VGS<VT)
VT1
Exponential
Quadratic
1 decade
VT2
VT3
VGS
log IDS
IOFF
~80 mV
For example:
If we suppose VT=0,3V
0,3V/80 mV=3,75
ION/IOFF = 103,75 ~ 5600
If VT=0,6V, ION/IOFF >107 !!
ION
OF COURSE WE WANT  CLOSE TO UNITY

## Slide 77: Short channel MOSFETs
  Threshold voltage reduction
  Drain Induced Barrier Lowering (DIBL)
  Channel length modulation
  MOSFETs breakdown
  …

## Slide 78: Threshold voltage reduction: short channel effect (Kang et al)
Origin:
  Previous VT expression supposes channel depletion region comes only from gate
  In fact one part is created by depletion region associated by source/channel and drain/channel pn junctions
  Overestimation of charge induced by gate  overestimation of VT
This reduction more prominent for MOSFET with shorter channel length

## Slide 79: Threshold voltage reduction: short channel effect (Kang et al)
Origin:
  Previous VT expression supposes channel depletion region comes only from gate
  In fact one part is created by depletion region associated by source/channel and drain/channel pn junctions
  Overestimation of charge induced by gate  overestimation of VT
This reduction more prominent for MOSFET with shorter channel length

## Slide 80: Threshold voltage reduction: short channel effect (Kang et al)

## Slide 81: Threshold voltage reduction: short channel effect (Kang et al)
Threshold voltage is function of:
  Channel length
  Drain –Source voltageVds through xdD
0
1
2
3
4
5
6
0,3
0,4
0,5
0,6
0,7
0,8
0,9
V
T0
Threshold voltage (V)
Channel Length (µm)

## Slide 82: Drain Induced Barrier Lowering (DIBL)

## Slide 83: Channel length modulation (saturation operation)
At the onset of pinch-off (VDS>VDsat), the effective channel length (the length of inversion layer) is reduced.

## Slide 84: MOSFET Breakdown
2 main effects:
  punchthrough breakdown
    Punch through in a MOSFET is an extreme case of channel length modulation where the depletion layers around the drain and source regions merge into a single depletion region.
    Punch through causes a rapidly increasing current with increasing drain-source voltage
    No current saturation
  Impact ionisation at the drain:
    Electron acceleration in the channel
    Impact ionisation  holes electrons pairs
    generated
    Holes collected by substrate  substrate current
     voltage drop in the channel
    Reduction of VT ( body effect)
    Increase of current and so on !
    Permanent dammage

## Slide 85: MOSFET capacitances
Difficulties:
  In general, capacitances associated with MOS circuits are a complicated function of geometries and process
  Not lumped capacitances but distributed capacitances
In the following, first approximation model
  Sufficiently accurate to represent main characteristics of MOSFET charge voltage behavior
  All the capacitances are lumped
Three differents physical origins
  Overlay capacitance
  Oxyde capacitance
  Junction capacitance
  Important point : capacitances are dependent of bias voltage / working point.

## Slide 86: MOSFET capacitances
Overlay capacitances:
  LD, gate – drain and gate – source overlay
  LM, mask length
LM
L
LD
LD
(n+)
(n+)
gate
L=LM - 2.LD
W

## Slide 87: MOSFET capacitances
Cdb
MOSFET
(DC Model)
Cgb
Cgd
Cgs
Cdb
Csb
S
D
G
B
Lumped representation of parasistics capacitances
Equivalent model (with overlap capacitances)

## Slide 88: Gate – Channel capacitances
channel
channel
Cut off mode:
Linear mode
Saturation mode
Cgs = Cgd = 0
Cgb = CoxWL

## Slide 89: Oxyde capacitance
Capacitance | Cut off | Linear | saturation
Cgb(total) Cgd(total) Cgs(total) | CoxWL CoxWLD CoxWLD | 0 | 0

## Slide 90: Dynamic characteristics (1)
Conductance:
  Linear mode
  Saturation mode

## Slide 91
transconductance: device speed
  linear
  « active region »
Dynamic characteristics (2)

## Slide 92: HF Caracteristics
Cut off frequency current gain = 1
If we neglect jwRLCgd (small)
CM : Miller capacitance

## Slide 93: HF Caracteristics
If CM = 0 (or minimum)  cut off frequency is maximum (saturation mode):
or (if short chanel and/or vsat )

## Slide 94: HF Caracteristics
An other figure of merit : power gain =1  oscillation frequency
Ref: (Tsividis)
Rg: gate resistance
Rs : negligeable

## Slide 95: MOS transistors InverTERS
Statics characteristics

## Slide 96: ideal Inverter : definition
Input voltage: Vin
Output voltage: Vout
Inverter threshold voltage:Vth=VDD/2
Logic « 1 » output :
  0<Vin<Vth
Logic « 0 » output:
  Vth< Vin <VDD
Vertical drop in ideal case

## Slide 97: NMOS Inverter: general circuit structure
Load: active (MOS) or passive (resistor)
« driver »
Cload :lumped capacitance
Input Voltage: Vin=Vgs
Output Voltage: Vout=Vds
DC domain: no input current neither output current
Kirchoff’s current law: ILOAD(VL) = IDS(Vin, Vout)

## Slide 98: Inverter: voltage transfer characteristics
With analytical solving
IDS ( Vin ,Vout )=IL( VL ) we found the VTC characteristics:
Vout = f ( Vin )
Key voltages:
  VIL : maximum input voltage wich can be interpreted as a « 0 » logic input
  VIH : minimum input voltage wich can be interpreted as a « 1 » logic input
  VOL : minimun ouput voltage when the output level is logic « 0 »
  VOH : maximum ouput voltage when the output level is logic « 1 »

## Slide 99: Inverters: noise margins
Interconnexions and gate noise can add parasitics voltage  logic faults . We introduce for quantify the noise immunity of the circuit the «noise margins ».
The noise immunity increases with the noise margins

## Slide 100
Uncertainty region must be reduce we must have VIL~VIH
 VTC close to ideal inverter
VOH’
VOL’
Inverters: noise margins

## Slide 101
Preceding discussions of inverter static (DC) characteristics show that shape of the VTC in general and noise immunity in particular are very important criteria for design priorities.
  For any inverter circuit five critical points (VIL, VIH,…) fully determine the properties.
  Accurate estimation of these voltage points have to be determined.
Inverters: brief summary

## Slide 102: Resistive-load Inverter
Vin=VGS
  Vin=« 1 »: n-MOS is ON  at first order, Drain grounded Vout = « 0 »
  Vin=« 0 »: n-MOS is OFF  open circuit  IL = IDS = 0  Vout= VDD= « 1 »
CL
RL
Input Voltage Range | Operating Mode
Vin<VT0 | Cut off
VT0<Vin<Vout+VT0 | Saturation
Vin>Vout+VT0 | Linear

## Slide 103: Resistive-load Inverter : VTC

## Slide 104: Resistive-load Inverter : VTC
( good exercise ! )

## Slide 105: Saturated enhancement-type nMOS Inverters :
VGS = VDS  VGS -VT < VDS  saturation mode
Warning : if Vout>VDD-VT  cut-off VOH=VDD-VT

## Slide 106: Saturated enhancement-type nMOS Inverters : graphic analysis
The representative points of the load line are given by :
VGS = VDS
The load NMOS is equivalent to a non linear resistance
VDS
VGS
Non linear resistance

## Slide 107: Saturated enhancement-type nMOS Inverters : graphic analysis
VDS1=VDD - VDS2 = 6 - VDS2
VDS1 = 6 – 4 = 2 V
ID2 = 75 µA = ID1
ID2, µA
VDS2
4
75
75
2
Load
Driver

## Slide 108: Saturated enhancement-type nMOS Inverters : graphic analysis
NMH = VOH -VIH = -0.2 V <0
By changing the ratio W/L, we can improve NM.
75
2
B

## Slide 109: Inverter with linear enhancement type load
Load transistor never in saturation mode:
  VGS,load – VT,load >VDS,load (1)
  VGS,load –VDS,load = VGG – VDD
  (1) OK  VGG – VDD >VT,load
  non saturated load
drawback : 2 separated power supply voltage !!

## Slide 110: Inverter with linear enhancement type load
VGS2 - VDS2 =VGG – VDD = 3V
VDS2 = VGS2 – 3V
T2
T1
VGG = +9V VDD = +6V
VGS1
VDS1
Load
resistance
Load
resistance

## Slide 111: Inverter with linear enhancement type load
VDS1 = 6 – VDS2

## Slide 112: Depletion Load NMOS inverter
Driver : enhancement  VT,Driver >0
Load : depletion  VT,load <0  VGS,load =0 >VT,load
VSB,load = VDS,pilote = Vout  VT,load sensitive to body effect
VDD = +6V
Vin | Vout | Driver | load
VOL | VOH | Cut off | Linear
VIL | ~VOH | Saturation | Linear
VIH | small | Linear | Saturation
VOH | VOL | linear | saturation

## Slide 113: Depletion Load NMOS inverter
VDS2 = 0 V, IDS2 = 0 µA
VDS1 = 6 – 0 = 6 V
VDS2 = 3 V, IDS2 = 22 µA
VDS1 = 6 – 3 = 3 V

## Slide 114: Depletion Load NMOS inverter
( good exercise! )
Drawback (compare to enhancement load Inverter):
Additional processing step (VT adjust for load)
Advantages (compare to enhancement load Inverter):
Sharp VTC transition
Better noise margins
Single power supply
Smaller layout area

## Slide 115: Depletion Load NMOS inverter: power considerations
Vin = 0 et Vout = VOH  driver is cut off  IDS=0. No power
Vin= VDD et Vout = VOL  both transistors ON  large current
unacceptable
50% of time logic« 1 »

## Slide 116: C-MOS inverter
All previous Inverters are based on :
  enhancement driver NMOS
  a load which can be a resistor, an enhancement or depletion NMOS.
Major drawback: in one state (output level « 0 ») DC consumption or power dissipation nonzero
New concept /design :
  One enhancement NMOS and one enhancement PMOS (Complementary MOS or CMOS).
  Depending on input Voltage, NMOS is the load and PMOS the driver and vice versa.
  Advantages:
    No DC ( steady state) power dissipation ( except leakage current)
    Full output voltage swing between VDD and 0
    Very sharp VTC transition : very similar to ideal inverter

## Slide 117: C-MOS inverter
S
S
D
D
VGS,p | -(VDD – Vin)
VDS,p | -(VDD – Vout)
VGS,n | Vin
VDS,n | Vout

## Slide 118: C-MOS inverter
The structure complexity of CMOS is the price to be paid for the improvements achieved in power consumption and the noise margins

## Slide 119: C-MOS inverter
VTn > 0 et VTp < 0
1st case: Vin < VTn
  VGS,n < VTn  nMOS cut off zero current
  VGS,p < VTp  pMOS ‘ON ‘ Vout = VDD = VOH
2nd case: Vin > VDD + VTp
  VGS,n > VTn  nMOS ‘ON ’ zero current
  VGS,p > VTp  pMOS cutoff Vout = VOL = 0

## Slide 120: C-MOS inverter

## Slide 121: C-MOS inverter
Region | Vin | Vout | nMOS | pMOS
A | < VTn | VOH | Cut off | linear
B | VIL | « 1 » VOH | Saturation | linear
C | Vth | Vth | Saturation | Saturation
D | VIH | « 0 » VOL | linear | Saturation
E | > (VDD + VT,p ) | VOL | linear | Cut off
Consumption zone when switching

## Slide 122: C-MOS inverter

## Slide 123: C-MOS inverter: switching characteristics
Interconnect effects
Cint represents the parasitic capacitance between the two inverters

## Slide 124: C-MOS inverter: switching characteristics
To simplify the problem, all the capacitances are combined into a unique lumped linear capacitance Cload
The question of inverter transient response is reduced to finding the charge-up and charge-down time of a single capacitance which is charged and discharged through a transistor (NMOS or PMOS).
Cload

## Slide 125: C-MOS inverter: switching characteristics
Delay-time or Propagation-time:
tPLH : delay time from « 0 » to « 1 ».
tPHL : delay time from « 1 » to « 0 ».
The average propagation delay time :

## Slide 126: C-MOS inverter: switching characteristics
VOL
VOH
Output voltage Rise and Fall time:

## Slide 127: C-MOS inverter: switching characteristics
Calculation of delay times:
Fall time calculation:
  Vin switches from VOL to VOH
  nMOS is turned ‘ON’ and it starts to discharge Cload
  pMOS is switched off ID,p 0

## Slide 128: C-MOS inverter: switching characteristics
Be carefull : during the switching, operating mode of MOS changes !!
In our case , we have to decompose the calcul in two delay-times
NMOS in saturation ?
VGSn – VTN < VDS  Vin-VTN <Vout  VOH – VTn < Vout

## Slide 129: C-MOS inverter: switching characteristics
After few steps

## Slide 130: C-MOS inverter: switching characteristics
Other method (more simple, less accurate): average current method

## Slide 131: C-MOS inverter: switching characteristics
Power dissipation for a gate CMOS during switching : this is the power used to charge and discharge the capacitance Cload.

## Slide 132: C-MOS inverter: switching characteristics
Another source of power consumption: the short-circuit current, ie a direct pathway from power supply to ground through PMOS and NMOS, both of them being in “ON” state.

## Slide 133: bibliographic references
S.M. Sze « Physics of semiconductors devices », 2° edition, Wiley and Sons, New York, 1981
H.Mathieu, « Physique des semi-conducteurs et des composants électroniques », 4° edition, Masson 1998.
J. Singh, « semiconductors devices : an introduction », McGraw-Hill, Inc 1994
D.A. Neamen, « Semiconductor physics and devices », McGraw Hill, 2003
Y.Taur et T.H. Ning, « Fundamentals of Modern VLSI devices », Cambridge University Press, 1998.
K.K. Ng, « complete guide to semiconductor devices », McGraw-Hill, Inc, 1995
E. H. Nicollian et J. R. Brews, « MOS Physics and Technology », John Wiley and Sons, 1982
S.M. Kang et Y. Leblebici, « CMOS Digital Integrated Circuits : analysis and design », Mc Graw Hill, 2° edition., 1999
J. Millman et A. Grabel, « microelectronique », Mc Graw Hill, 1995
Chenming C. Hu « Modern Semiconductor Devices for Integrated Circuits », Prentice Hall, 2009
Figures and tables mainly from these references

## Slide 134: MERCI! Thank you for your attention!
感谢您的关注